## Module 02108-05
Cast-Iron Pipe and Fittings

Lesson 2 of 3: Measuring, Cutting, and Joining

This lesson is a classroom and lab session in which the students will learn how to measure, cut, and join cast-iron piping.  Students will select appropriate personal protective equipment for working with cast-iron piping, and then measure, cut, and join cast-iron pipe to fulfill Performance Task requirements.

Objectives

Upon completion of this lesson, the student should be able to:

- Identify the hazards and safety precautions associated with cast-iron piping.

- Demonstrate the ability to properly measure, cut, and join cast-iron piping.

- Identify the tools and materials required to create lead and oakum joints.

- Identify the tools and materials required to join sections of no-hub pipe.

Performance Requirements

  - Select appropriate personal protective equipment for working with cast-iron piping.  This corresponds to Performance Task 3.

  - Measure, cut, and join cast-iron piping. This corresponds to Performance Task 4.

Reading Assignment

  - Module 02108, Section 4

Slide Presentation

  - Module 02108, Part 2 (Slides 17 thru 41)

Suggested Equipment/Materials

  - Materials and tools needed to measure, cut, and join cast-iron piping.

Suggested Student Activity

  - Students will view a video on joining cast-iron piping.

Testing

  - Module Review Test Questions 1 thru 8 for Section 4.0.0.

  - CONTREN( Connect, Active Figure 22

Suggested Lab Activity

  - Students must select appropriate personal protective equipment for working with cast-iron piping, and measure, cut, and join cast-iron piping.

Additional Resources

  - Installation Suggestions for No-Hub Pipe and Fittings, Washington. DC, Cast Iron Soil Pipe Institute.

  - www.acipo.com/adip/pdfandvideo.cfm (American Ductile Iron Pipe) Downloadable videos and PDF files dealing with assembly of ductile iron pipe systems.

  - Contren Connect Level 1Plumbng Annotated Instructors Guide (available from the NCCER)

SLIDE 17

  - Review the objectives to be covered in this lesson.  Ask students if they have any questions about the lesson or course objectives.

  - Explain that measurement is critical when cutting pipe to make a lead and oakum joint.

  - Explain that the insertion length of a pipe into a fitting must be taken into account when measuring pipe for cutting.

SLIDE 18

  - Explain the importance of knowing how to locate the center of a fitting.  Describe and demonstrate how it is done.

SLIDE 19

  - Describe and demonstrate how to determine the length of pipe that goes between two fittings.  Use slides 19 & 20 (Figures 16 & 17).

  - Provide students with example measurements and have them determine the cutting length.

SLIDE 20

No notes

SLIDE 21

  - Describe and demonstrate how to use a folding rule to find the length of pipe to be cut.

  - Allow students to practice this procedure.

SLIDE 22

  - Describe and demonstrate how to cut cast-iron pipe with a soil pipe cutter.

  - Allow students to practice cutting pipe with this tool.

SLIDE 23

  - Describe and demonstrate how to measure no-hub pipe for cutting.

  - Allow students to practice this procedure.

SLIDES 24

  - Explain that hub-and-spigot pipe can be joined by two methods:  the compression joint and the lead and oakum joint.

  - Describe and demonstrate the steps for creating a compression joint.  See paragraph 4.3.1.

  - Allow students to create a compression joint.

SLIDE 25

- Describe how a lead-and-oakum joint is made.

SLIDE 26

  - Describe and demonstrate how a running rope and a spring clamp are used to hold molten lead in place to create a horizontal joint.

  - Allow students to use a running rope and spring clamp to prepare a joint for the pouring of lead.  Note:  DO NOT pour lead at this point in the lesson.

SLIDE 27

No notes

SLIDE 28

  - Discuss the furnace used for melting lead

  - Review the safety precautions for working around molten lead.

  - Ask students to describe the personal protective gear that would be appropriate for use when pouring molten lead.

SLIDE 29

No notes

SLIDE 30

  - Describe and demonstrate how to use the various other hand tools that are required to make a lead and oakum joint.  See Slides 30 thru 36 (Figures 27 thru 33).

  - Have samples of the tools available to pass around the class.

SLIDE 37

  - Describe and demonstrate how to make a vertical lead and oakum caulked joint.

  - Under your supervision, allow students to practice this procedure.  Ensure that all parties involved are wearing the appropriate personal protective equipment.

SLIDE 38

  - Describe and demonstrate how to make a horizontal lead and oakum caulked joint.

  - Under your supervision, allow students to practice this procedure.  Ensure that all parties involved are wearing the appropriate personal protective equipment.

SLIDE 39

  - Describe and demonstrate how couplings are used to join no-hub pipe.

  - Have samples of couplings available to pass around the class.

SLIDE 40

  - Demonstrate how to use the special torque wrench to tighten clamps on no-hub pipe.

  - Allow students to tighten couplings on no-hub pipe using a torque wrench.

SLIDE 41

Have students answer Review Questions for Section 4.0.0. Provide correct answers and remediation at the end of the quiz.  Have students complete Active Figure 22.

Students must select appropriate personal protective equipment for cast-iron piping, and measure, cut, and join cast-iron pipe.  These tasks correspond to Performance Tasks 3 and 4 respectively.